KITCHEN SINKS

LAVATORY BOWLS

Tower Industries, Inc.

2101 Ninth St. SW, Massillon OH  44647

330.837.2216

www.TowerSinks.com

PART 1 – GENERAL

1.1 RELATED SECTIONS

- Related work specified in other sections:

01 33 00	“Submittal Procedures”

06 61 16	“Solid Surfacing Fabrications”

12 36 61.16 	“Solid Surface Countertops”

22 42 16	“Commercial Lavatories and Sinks”

22 43 16	“Healthcare Sinks”

1.2 REFERENCES

- Codes and Standards referenced in this section refer to the latest edition thereof.

- Applicable Standards referenced herein:

ASTM: American Society for Testing and Materials

ANSI: American National Standards Institute

NSF: National Sanitation Foundation

1.3 SUMMARY

- Section includes:

Meridian Solid Surface® material, as indicated and specified

- Work Specified in this Section:

Single-Bowl Kitchen Sinks

Double-Bowl Kitchen Sinks

Triple-Bowl Kitchen Sinks

Lavatory Bowls

1.4 DEFINITION

- Solid surface is a homogeneous thermoset polymer compound, comprised of acrylic and polyester components blended with pigments and/or mineral fillers and filled with alumina trihydrate. Material is non-porous and homogenous, with uniform color and pattern throughout the entire thickness.

  - SUBMITTALS

- Submit color samples for product verification, 2”x2”x1/2” nominal

- Submit samples of full range of available colors for color selection

- Care & Maintenance Data

Provide manufacturer’s care and maintenance instructions

  - DELIVERY, STORAGE AND HANDLING

- Transport and deliver all items in appropriate packaging to prevent damage.

- Handle materials to prevent damage to adjacent surfaces and previous work.

1.7 QUALITY ASSURANCE

- Source Limitations

Where solid surface sinks, kitchen sinks, or lavatory bowls are indicated on drawings, the material shall be Meridian Solid Surface®, manufactured by Tower Industries, Inc., 2101 Ninth St. SW, Massillon, OH  44647. Phone 330.837.2216

- Installation Qualifications

Meridian Solid Surface® products shall be installed in accordance with standard industry practice and utilizing manufacturer’s recommended adhesives, means, and methods.

1.8 WARRANTY

- Furnish the manufacturer’s Limited Ten-Year Warranty covering defects in material and workmanship. Term of warranty to commence upon date product is delivered to the jobsite.

PART 2 - PRODUCTS

2.1 MANUFACTURER

Tower Industries, Inc.

2101 Ninth St. SW, Massillon OH  44647

330.837.2216

www.TowerSinks.com

2.2 MATERIALS

- Solid Polymer Fabrications

  - Solid surface material shall be Meridian Solid Surface®, manufactured by Tower Industries, Inc., 2101 Ninth St. SW, Massillon, OH  44647. Phone 330.837.2216

  - Solid surface material shall be a homogeneous thermoset polymer compound comprised of acrylic and polyester components blended with pigments and/or mineral fillers and filled with alumina trihydrate. Materials shall be non-porous and homogenous, with uniform color and pattern throughout the entire thickness. Materials shall be 100% repairable.

  - Solid surface material shall meet or exceed all performance requirements listed in Section F below.

  - All products shall carry a Limited Ten-Year Warranty covering defects in material and workmanship.

- Products

  - Single-Bowl Kitchen Sinks

    - Single-bowl kitchen sinks shall be Meridian Solid Surface®, manufactured by Tower Industries, Inc., 2101 Ninth St. SW, Massillon, OH  44647. Phone 330.837.2216

    - Single-bowl kitchen sinks shall be manufactured from solid cast polyester/acrylic blend resin and have fixed drain locations.

    - Single-bowl kitchen sinks shall have a nominal 3½” diameter drain orifice to accept a standard basket strainer assembly.

    - Single-bowl kitchen sinks shall meet the minimum ANSI Z124.6 certification.

    - Single-bowl kitchen sink model(s) shall be as follows:

      - #160 Large Single Bowl, Model MKS160

      - #200 Small Single Bowl, Model MKS200

      - #210 Single Bowl, Model MKS210

      - #215 Single Bowl, Model MKS215

      - #220 Single Bowl, Model MKS220

      - #230 Single Bowl, Model MKS230

  - Double-Bowl Kitchen Sinks

    - Double-bowl kitchen sinks shall be Meridian Solid Surface®, manufactured by Tower Industries, Inc., 2101 Ninth St. SW, Massillon, OH  44647. Phone 330.837.2216

    - Double-bowl kitchen sinks shall be manufactured from solid cast polyester/acrylic blend resin and have fixed drain locations.

    - Double-bowl kitchen sinks shall have a nominal 3½” diameter drain orifice in each bowl to accept a standard basket strainer assembly.

    - Double-bowl kitchen sinks shall meet the minimum ANSI Z124.6 certification.

    - Double-bowl kitchen sink model(s) shall be as follows:

      - #100 Equal Double Bowl, Model MKS100

      - #101 Equal Double Bowl, Model MKS101

      - #104 Uneven Double Bowl, Model MKS104

      - #150 Equal Double Bowl, Model MKS150

  - Lavatory Bowls

    - Lavatory bowls shall be Meridian Solid Surface®, manufactured by Tower Industries, Inc., 2101 Ninth St. SW, Massillon, OH  44647. Phone 330.837.2216

    - Lavatory bowls shall be manufactured from solid cast polyester/acrylic blend resin and have fixed drain locations.

    - Lavatory bowls shall have a nominal 1½” diameter drain orifice to accept a standard drain assembly.

    - Lavatory bowls shall meet the minimum ANSI Z124.3 certification.

    - Lavatory bowl model(s) shall be as follows:

      - #51 Small Oval with Overflow, Model MLB051

      - #60 ADA, Model MLB060

      - #75 “Wave”, Model MLB075

      - #98 Standard Oval with Overflow, Model MLB098

- Color

  - Kitchen Sink / Lavatory Bowl Color

    - To be selected from manufacturer’s standard selection of solid colors

- Finish

  - All products to be supplied in Matte Finish

- Basic Limitations

  - Material designed for interior use only.

- Performance Characteristics

  - Comprehensive Analysis Data - Meridian Solid Surface®

| Test Type | Test Method | Meridian Tested Results |
| --- | --- | --- |
| Hardness | ASTM D-2583-95 | 58- 62 |
| Tensile Strength | ASTM D- 638 | 3520 psi |
| Tensile Modulus |  | 11 x 105 |
| Gloss | NEMA LD 3-3 1513.2 | 5- 20 |
| Wear and Clean | ANSI Z124.3 | Passes |
| Abrasion Resistance | ASTM C501 | 0.9 grams @ 1000 cycles |
| Cigarette Resistance | NEMA LD3-3.07 | No Effect |
| Boiled Water Resistance | NEMA LD3- 3.05/3.5 | See Below* |
| High Temperature Resistance | NEMA LD3- 3.06/3.5 | No Effect |
| Chemical Resistance | ANSI Z124.3 | No Effect |
| Colorfastness | ASTM D-2565 | No Effect |
| Conductive Heat | NEMA LD3- 3.08/ 3.8N | No Effect |
| Stain Resistance | ANSI Z124.3 | Passes- 26 |
| Water Absorption | ASTM D- 570- 95 | 0.022 |
| Flammability | ASTM E- 84 | Class 1 |
| Impact Resistance | NEMA LD3-3.3 | No fracture |
| % Cure by DSC | Analytical | 99% |
| Shower Receptor | ANSI Z124.2 | PASS |

* Boiling water and high temperature resistance tests may have an effect on the surface;

however, the surface can be renewed to ‘No Effect’.

  - Fire Test Data

    - Solid Surface materials shall be classified by Underwriters Laboratories under UL File Number R14436 for surface burning characteristics.

    - Test data for Solid Surface panels shall be generated according to ASTM E 84: Standard Test Method for Surface Burning Characteristics of Building Materials. This procedure is catalogued by Underwriters Laboratories, Inc. as UL 723. For panels with a thickness of one-half inch (13 mm), the Flame Spread Index is less than or equal to 25 and the Smoke Developed Index is less than or equal to 25.

  - Materials shall comply with the following Codes

    - Approved by NSF International Standard 51 “Splash Zone” areas.

    - ASTM G-22 bacterial resistance

    - ASTM G-21 fungal resistance

PART 3 - EXECUTION

3.1 EXAMINATION

- Examine all substrates to which the kitchen sink or lavatory bowl will be attached for compliance with established tolerances and other conditions affecting performance of work.

- Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 INSTALLATION

- Attach kitchen sinks or lavatory bowls to specified countertop material in shop in accordance with standard industry practice.

  - Utilize manufacturer’s recommended adhesives.

  - Do not cut, notch, or otherwise modify kitchen sink or lavatory bowl

- Coordinate countertop materials and installation details with Division 12.

- Coordinate plumbing installation with Division 22.

3.3 CLEANING

- Keep components clean during installation.

- Remove all adhesives and sealants from the product surfaces.

- After installation is complete, remove all excess adhesive, dirt and debris from the installation area.

3.4 PROTECTION

- Protect surfaces from damage until project is completed. Repair or replace damaged components which cannot be repaired to the Architect’s satisfaction.