Technical Data Sheet

NECAL 8495  PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8495 is a supported pressure sensitive adhesive displaying excellent tack.

FEATURES

8495 will adhere to many substrates.  8495 is highly recommended for rough textured surfaces that have low contact areas.  It can be used where vibration deadening is required.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P or W liner

Thickness:			 			32 mils + or – 10% (total)

Scrim:							30 mil polyurethane open-celled foam

Adhesion: (1)						95-120 oz./in.

Tensile: (2)						90 p.s.i.

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

300°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-10