Technical Data Sheet

NECAL 8517 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8517 is a supported pressure sensitive adhesive with a general purpose modified acrylic on one side and a general purpose acrylic on the other side displaying high tack.

FEATURES

8517 is designed for low energy surfaces (i.e. polyethylene and polypropylene) utilizing the acrylic side of the system.  The modified acrylic side should be bonded to the nameplate only.

PHYSICAL PROPERTIES

Composition:						General purpose acrylic on one side and a modified acrylic

on the other side

Release Liner:						Available with H, P or W liner

Thickness:			 			6.2-7.0 mils total

Scrim:							1 mil polyester

Adhesion: (1)						80-100 oz./in. (Aluminum/Polypropylene)

Tensile: (2)						220-250 oz./in.

Shear Adhesion: (3)					24 hours +

Temperature Range:					Application:	50°F. Minimum

Service:	-20°F. Minimum

195°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is  two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09