Ultra Heat Shrink Wrap FR 9 Mil

**Flame Retardant White with UVI**

**Product Description**

Ultra Heat Shrink Wrap FR 9 mil is suited for heavy-duty applications where excellent two directional shrink properties and toughness is required. Our Shrink-Warp is formulated from premium grade polyethylene, UV inhibitors, and other additives, which are designed to resist

 degradation due to sunlight, rain, chemicals, and heat. GPS Heat Shrink-

Warp is manufactured to the highest QC standards and is backed

by a proven track record of success.

|  |  |  |  |
| --- | --- | --- | --- |
| **TEST DESCRIPTION** | **METHOD** | **UNITS** | **9MIL FLAME/SHRINK****Nominal Value** |
| **Thickness** | **ASTM D374** | **Mil** | **9** |
| **Tensile Properties** | **ASTM D882** | **psi** | **1400/1200** |
| **-Yield (md/cd)** |
| **-Break (md/cd)** | **psi** | **2500/2400** |
| **-Elongation (md/cd)** | **%** | **600/700** |
| **Dart Impact** | **ASTM D1709** | **grams** | **750** |
| **Elmendorf Tear (md/cd)** | **ASTM D1922** | **grams** | **1200/1500** |
| **Shrink Temperature** | **ASTM D2732** | **degree F** | **275** |

MEETS WITH THE REQUIREMENTS OF

NFPA 701-15 Test 1