Poly Scrim 8 FR is a 3-ply, 8 mil extrusion laminate combining two layers of fire retardant,  low density polyethylene and a high-strength cord grid.  It is specifically engineered to provide high strength and durability in a lightweight material.

- Multiple layers and cord reinforcement resists punctures and tears.

- Grommets, tie-downs, hems, zippers, drains and 3-D custom shapes available.

- Flexibility and light weight allow for easy handling and quick installation

- Custom fabrication is available to meet your exact specification.

- Cold-crack resistance eliminates failures in extreme cold temperatures.

- Low permeability greatly inhibits moisture transmission.

- Long life expectancy allows for significant savings through reuse and fewer replacements.

- Colors:  Yellow and Natural

| Property | ASTM TEST METHOD | U.S. VALUE | METRIC VALUE |
| --- | --- | --- | --- |
| Weight | D-3776 | 30 LB/1000FT² | 14.6 KG/100 M² |
| 3” Tensile Strength | D-882 | 86 LBF | 356 N |
| Puncture Strength | D-4833 | 36 LBF | 160 N |
| PPT Resistance | D-2582 | 25 LBF | 111 N |
| Dart Impact Strength | D-1709 | 1.05 LBS | 480 g |
| Cold Impact Strength | D-1790 | -15˚F | -27˚C |
| Permeance | E-96 | 0.035 Grain/HR∙R²∙in.Hg | 2.011 NG/(PA∙S∙M² |
| Fire Retardancy | E-84 | 5 flame spread, 70 smoke developed |  |
|  | NFPA 701 | PASS |  |

SUGGESTED APPLICATIONS:

- Temporary walls, plant dividers, building enclosures and containment tents.

- Architectural vapor retarders in walls, ceilings and roofing systems.

- Floor covers, dust partitions and clean room enclosures.

- Pallet, cask and drum covers for outside storage.

- Shipping container covers and liners.