Poly Scrim 12 FR is a 3-ply, 12 mil extrusion laminate combining two layers of fire retardant PVC film and a high-strength cord grids.  It is specifically engineered to provide high strength and durability in a lightweight material.

# FEATURES

- Multiple layers and cord reinforcement resists tears.

- Grommets, tie downs, hems, zippers, drains and 3-D custom shapes available.

- Flexibility and light weight allow for easy handling and quick installation

- UV stabilization protects the material from degradation during extended exposure to sunlight.

- Custom fabrication is available to meet your exact specification.

- Passes NFPA 701 Large Scale-"Standard Methods of Fire Test for Flame-Resistant Textiles and Films".

- COLORS:  Green and Natural

| Property | ASTM TEST METHOD | U.S. VALUE | METRIC VALUE |
| --- | --- | --- | --- |
| Weight | D-751 | 54 LB/1000FT² | 26.3 KG/100M² |
| 3” Tensile Strength | D-882 | 80 lb/1000FT² | 356 N |
| 3” Load @ Break | D-882 | 40 LBF | 178 N |
|  |  | 1850 PSI | 13 MPA |
| 3” Elongation @ Break | D-882 | 150 % | 150 % |
| Tongue Tear | D-2261 | 13 LBF | 58 N |
| Trapezoidal Tear | D-4533 | 18 LBF | 80 N |
| PPT Resistance | D-2582 | 24 LBF | 106 N |
| Dart Impact Strength | D-1709 | 28 LBS | 1250 g |
| Cold Impact Strength | D-1790 | -10˚F | -12˚C |
| Fire Retardancy | E-84 | 15 flame spread, 250 smoke developed |  |
|  | NFPA 701 | PASS |  |

SUGGESTED APPLICATIONS:

- Temporary walls, plant dividers, building enclosures and containment tents.

- Floor covers, dust partitions and clean room enclosures.

- Equipment covers.

- Pallet, drum and other custom covers for outside storage.

- Shipping container covers and liners.