Technical Data Sheet

NECAL 4800 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

4800 is an unsupported film of pressure sensitive adhesive which displays excellent bond and initial tack.

FEATURES

4800 adheres to most substrates, including aluminum, brass, steel, glass, enamels and plastics such as polystyrene, ABS and acrylic.  Because of its thickness, 4800 is recommended for use on rough surfaces.

PHYSICAL PROPERTIES

Adhesive:						Acrylic

Release Liner:						P, P1,W,W1

Adhesive Thickness:					1.0 – 4.0 mils dependent upon application

Scrim:							2 mil chrome, 2 mil brush chrome, 1 mil mylar,

2 mil mylar, and 4 mil mylar

Adhesion:						325 - 350 oz./in. at 4.0 mils

Tensile:						180 p.s.i.

Shear Adhesion:					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

225°F. Maximum

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least one year when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09