Technical Data Sheet

NECAL 8875 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8875 is a supported pressure sensitive adhesive displaying excellent tack.

FEATURES

8875 will adhere to many substrates.  8875 is highly recommended for rough textured surfaces that have low contact areas.  It can be used where vibration deadening is required.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P or W liner

Thickness:			 			32 mils + or – 10%

Scrim:							Polyurethane open-celled foam

Adhesion: (1)						75-90 oz./in.

Tensile: (2)						70 p.s.i.

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

225°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09