## Slide 2: Corial 200I
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
ICP-RIE capabilities over a variety of materials including silicon, silicon compounds, metals, InP and polymers
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Uses fluorine- and oxygen-based chemistries to provide leading edge etch rates and uniformities
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Adaptable to a wide range of substrate sizes:
wafer pieces, 1x2’’ to 7x2; 1x3’’ to 3x3’’; 1x4’’; 1x6’’; 1x8’’
Industry-leading uniformity for etching a variety of materials

## Slide 3: System description Corial 200I

## Slide 4: System description
General View
630
750
1080
190
600
360
490
420
COMPACT FOOTPRINT
Low CoO

## Slide 5: System description
Detailed View
Pumping system
(TMP 500l/s and dry pump 28 m3/h)
Chiller / Heater
ICP reactor
HV and LV power supplies
Process controller
2 kW ICP generator
(2 Mhz)
300W RF generator
(13,56 Mhz)

## Slide 6: System description
Loading
Direct loading on carrier
FAST LOAD AND UNLOAD
< 210 s
LOADING TIME
Shuttle
EASY EXCHANGE BETWEEN SUBSTRATE SHAPE AND SIZE

## Slide 7: Icp source corial 200I

## Slide 8: Icp source
CORIAL’s latest generation of reactor
High process flexibility with wide RF power operating range from 100 W to 2000 W
Exceptional uniformity, and repeatability enabled with a unique high-power ICP reactor with helical antenna
Uniform temperature control (from -50°C) for best repeatability
Reactor’s hot walls enhance plasma cleaning efficiency and reduce particle load
Retractable liner and shuttle holding to minimize process cross-contamination
Short pump-down cycle (<3 minutes), rapid reactor clean time (<20 minutes), and shuttle loading direct on the carrier, to guarantee high system uptime
HIGH PERFORMANCE AND FLEXIBILITY

## Slide 9: Icp source
Retractable Quartz Liner
1 min
Reactor Venting
4 min
Pumping down to 10-4 Tor
5 min
Liner replacement
5 min
Plasma cleaning
EASY LINER replacement by a single person
THE LINER FOR
HARSH ICP-RIE
PROCESSES
ZERO
CROSS CONTAMINATION

## Slide 10: Icp source
RF coupling to ICP source
Minimum parasitic capacitive coupling giving rise to low plasma potential to enable low damage etching
< 15
volts
SiO2 Isotropic etching with NO RF biasing
GaN Low damage etching with low RF biasing

## Slide 11: Icp source
Operation Sequence
Loading tool
Shuttle
Cathode
Shuttle Loading
1

## Slide 12: Icp source
Operation Sequence
Loading tool
Shuttle
Cathode
Cathode Up
2

## Slide 13: Icp source
Operation Sequence
Cathode
Loading tool
Shuttle
Helium
PLASMA
Coolant IN
Coolant OUT
Heat is transferred to shuttle and to the cooled cathode by He pressure at 5 Torr
Plasma heats wafer and clamping ring
3

## Slide 14: Icp source
Temperature Control
New cathode design and efficient helium back side cooling of the shuttle and substrate ensure uniform temperature control (from -50°C) during the etch process
Test based on 1 KW configuration for sapphire etching (1 X 2” wafers)
  No resist damage when operating at
  full ICP and RF power (Novolak type photoresist baked at 110°C)
Process | Etch rate | ICP Power | RF Power
Sapphire | 300 nm/min | 1 KW | 280 W

## Slide 15: Icp source
Reactor Uniformity
Benchmark uniformity test: 500 nm etching of thermal oxide (8” wafers)
  Remaining 100 nm measured by ellipsometry
  Measurement performed with 5 mm edge exclusion
Process | Etch depth | Uniformity | ICP Power | RF Power
Thermal SiO2 | 500 nm | ± 2.2% | 800 W | 150 W

## Slide 16: Shuttle holding approach corial 200i

## Slide 17: Shuttle holding approach
Benefits
Quick adaptation to sample shape and size
Optimum process conditions with NO modification of process chamber
Limited cross contamination between processes by using dedicated shuttles
Shuttles for single wafer treatment: 1 x 2”, 1 x 3”, 1 x 4”, 1 x 6”, 1 x 8”
Shuttles for batch processing : 7 x 2”, 3 x 3”
Customized shuttles are available (4” x 4”, 5” x 5”, etc)

## Slide 18: Shuttle holding approach
Portfolio
Clamping ring
Wafer
O’ring
Moving plate
Quartz shuttle
Wafers
Aluminum table
O’rings
  Guaranteed no wafer damage due to SOFT wafer clamping

## Slide 19: Performances icp-rie processes Corial 200I

## Slide 20: ICP-RIE of SI
Fluorinated chemistry
High Resolution ICP-RIE of Si
ICP-RIE of Si microlenses 40 µm high

## Slide 21: ICP-RIE OF OXIDES AND NITRIDES
Fluorinated chemistry
ICP-RIE of SiO2
ICP-RIE of SiO2 Microlenses
ICP-RIE of Si3N4

## Slide 22: ICP-RIE OF METALS & DIAMOND
Tapered ICP-RIE of Mo
ICP-RIE of Ta
ICP-RIE of Diamond

## Slide 23: ICP-RIE of inp
CH4/H2 chemistry
RIE of InP 0.1 µm lines and spaces
Deep RIE etching of InP

## Slide 24: High etch rates
Excellent Uniformities
Process | Mask | Etch rate (nm/min) | Selectivity (vs mask) | Uniformity (across wafer)
Polymers | PR | 800 | 1 | ±5%
Si | PR | 500 | > 5 | ±3%
SiO2 | PR | 400 | > 3 | ±3%
Si3N4 | PR | 350 | > 4 | ±3%
Diamond | SiO2 | 500 | > 25 | ±3%
InP | SiO2 | 1200 | > 25 | ±3%
Nb | PR | 250 | > 2 | ±3%
Ti | PR | 120 | 0.3 | ±3%

## Slide 25: Performances deprocessing processes corial 200I

## Slide 26: CONTROL OF SAMPLE TEMPERATURE
CORIAL’S advantage
OVERHEATING LEADS TO METAL LIFT OFF!
WITHOUT TEMPERATURE CONTROL
TEMPERATURE > 150°C
Tight control of sample temperature with helium backside cooling of wafer, dies and packaged dies
NO METAL LIFT
CORIAL LOW TEMP. DEPROCESSING
TEMPERATURE < 100°C
ELECTRICAL FUNCTIONALITY MAINTAINED
Al TECHNOLOGY
4 METAL LAYERS REVEALED

## Slide 27: Deprocessing on wafer
Delayering for advanced technology nodes
300 NM/MIN ETCH RATE
28 NM TECHNOLOGY
> 50:1 SELECTIVITY TO Al/Cu MASK
LOW-K DIELECTRIC ETCHING
200 NM/MIN ETCH RATE
20 NM TECHNOLOGY
> 50:1 SELECTIVITY TO Al/Cu MASK
ULTRA LOW-K DIELECTRIC ETCHING

## Slide 28: Deprocessing on wafer
Isotropic etching with NO RF biasing
Exposure of 7 metal levels (Cu technology)
Anisotropic etching with low RF biasing

## Slide 29: Deprocessing on wafer
3 metal level exposure (Al technology)
4 metal level exposure (Cu technology)
5 metal level exposure (Cu technology)

## Slide 30: Process performances
On Wafer
200 mm wafer
Process | Underlayer | Etch rate (µm/min) | Selectivity (vs. mask)
Polyimide | Si3N4 | > 1 | > 50
Si3N4 | SiO2 | > 0.3 | > 1.5
SiO2 | SiO2 | > 0.15 | -
SiO2 / TiN | TiN | 0.05 | > 10
Aluminum (load-lock required) | SiO2 | 1 | > 10
Titanium (load-lock required) | SiO2 | > 0.1 | > 2

## Slide 31: Performances sputter-etch processes Corial 200I

## Slide 32: Sputter-etch
Retractable Liner
Ni COATED LINER TO COLLECT SPUTTERED MATERIALS IN
METAL RIE SPUTTER-ETCH MODE
Pt SPUTTERING WITH PR MASK

## Slide 33: usability corial 200I

## Slide 34: Process control software
COSMA
The simplest, most efficient software to develop processes, operate, and maintain CORIAL systems
DESKTOP APPLICATION
Process Editing I Process Adjustment I Process Operation I Process Tracability I System Maintenance
REMOTE CONTROL
COSMA
CORIAL OPERATING SYSTEM FOR MACHINE

## Slide 35: Deprocessing software
COSMA RS
REMOTE
ANALYSIS OF RUNS
DISPLAY UP TO 4
PARAMETERS FROM A RUN
DRAG AND DROP
CURVES TO CHECK PROCESS REPEATABILITY
Simple and efficient software to analyze process runs and accelerate process development

## Slide 36: End point detection
Real-Time etch rate measurement
Real-Time etched depth measurement
EPD with laser
A CCD camera and laser diode, in the same measuring head, enables simultaneous visualization of the wafer surface and the laser beam impact on it. A 20 µm diameter laser spot facilitates the record of interference signals.

## Slide 37: Corial 200I
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
ICP-RIE capabilities over a variety of materials including silicon, silicon compounds, metals, InP and polymers
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Uses fluorine- and oxygen-based chemistries to provide leading edge etch rates and uniformities
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Adaptable to a wide range of substrate sizes:
wafer pieces, 1x2’’ to 7x2; 1x3’’ to 3x3’’; 1x4’’; 1x6’’; 1x8’’
Industry-leading uniformity for etching a variety of materials