## Slide 1
DRIE APPLICATIONS
In Corial 210IL

## Slide 2: Corial 210IL
ICP-RIE equipment for deep etching applications
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Wide process range for silicon, silicon carbide, glass, sapphire, and quartz deep etch
Support time-multiplexed processes (Bosch) in conventional dry etch reactor
Smaller wafer pieces up to full 200 mm wafer

## Slide 3: performances glass drie process on corial 210IL

## Slide 4: Drie of glass
NO ROUGHNESS
> 800 NM/MIN
ETCH RATE
> 15 SELECTIVITY TO Ni MASK
± 3 %
UNIFORMITY
+30% ETCH RATE IMPROVEMENT OVER STANDARD PROCESS
> 100 µm ETCH DEPTH
CATHODE OPTIMIZED FOR Ni MASK CLAMPING

## Slide 5: performances SIC drie process on corial 210IL

## Slide 6: Sic via etch process with ni mask
ANISOTROPIC ETCH PROFILE
> 1400 NM/MIN
ETCH RATE
> 20 SELECTIVITY TO Ni MASK
± 3 %
UNIFORMITY
SMOOTH
SIDEWALLS
> 100 µm ETCH DEPTH

## Slide 7: performances Si drie process on corial 210IL with cosma pulse software

## Slide 8: COSMA Pulse is a control software that broadens conventional tools’ process capabilities to enable time-multiplexed processes

## Slide 9: Cosma pulse description
Advanced Process Control
ALL PARAMETERS
CAN BE CONTROLLED AND PULSED
EASY
recipe programation
10 ms
DATA AQUISITION
+/-0,1%
ACCURACY
ON BIAS FINE TUNING

## Slide 10: Si drie on corial 210IL
CORIAL Bosch-like process has 3 steps
step 1 - Polymer deposition by C4F8 plasma
step 2 - Polymer etching by SF6 plasma
step 3 - Silicon etching with 20W of RF power, which was used to increase the silicon etching rate
To alternate between each step,
COSMA pulse software is required for pulsing consecutively C4F8 gas flow, SF6 gas flow, LF and RF power

## Slide 11: Drie of silicon
Precise control of the etch profile, fast etch rates, and excellent etch uniformity

## Slide 12: Drie of silicon
Various Aspect Ratios
Feature size (µm) | Etched depth (µm) | Aspect ratio | Etch rate (µm/min) | Mask | Selectivity (vs. mask)
Ø250 | Through wafer | 1:2 | > 3.0 | SiO2 | 330
Ø100 | 515 | 1:5 | > 2.9 | PR | 85
Ø20 | 280 | 1:14 | > 1.5 | SiO2 | 155
Ø5 | 180 | 1:35 | > 1.0 | SiO2 | 100
Results obtained with 100 mm wafer, 20% Si open area

## Slide 13: System description Corial 210IL

## Slide 14: System description
ICP source
960
750
360
1570
600
420
390
490
General View
30 %
SMALLER FOOTPRINT
THE MOST
COMPACT
MACHINE
ON THE MARKET

## Slide 15: System description
Detailed View
Pumping system
(TMP 500l/s and dry pump 110 m3/h)
Chiller / Heater
Load lock
EPD with laser
ICP reactor
HV and LV power supplies
Process controller
ICP generator
(2 Mhz)
RF generator
(13,56 Mhz)

## Slide 16: System description
Loading
Vacuum robot
FAST AND REPEATABLE LOAD AND UNLOAD
< 180 s
LOADING TIME
Shuttle
EASY EXCHANGE BETWEEN SUBSTRATE SHAPE AND SIZE

## Slide 17: ICP SOURCE corial 210IL

## Slide 18: ICP source
CORIAL’s Latest Generation of Reactor
Load lock to run fluorinated and chlorinated chemistries in the same process recipe
Load lock for stable and repeatable process conditions
RF match box with matching range up to 2000 W
Uniform temperature control (from -50°C) for best repeatability
Hot walls (>250°C) minimize polymer condensation for selective processes
Hot walls and retractable liner reduce clean time
Retractable liner and shuttle holding to minimize process cross-contamination
FAST AND UNIFORM ETCHING

## Slide 19: ICP Source
Retractable Quartz Liner
THE LINER FOR
HARSH ICP-RIE
PROCESSES
1 min
Reactor Venting
4 min
Pumping down to 10-4 Tor
5 min
Liner replacement
5 min
Plasma cleaning
EASY LINER replacement by a single person
ZERO
CROSS CONTAMINATION

## Slide 20: Shuttle holding approach corial 210IL

## Slide 21: Shuttle holding approach
Portfolio
Clamping ring
Wafer
Base plate
O’ring
Moving plate
Quartz shuttle
Wafers
Aluminum table
O’rings
  Guaranteed no wafer damage due to SOFT wafer clamping

## Slide 22: Shuttle holding approach
Benefits
Quick adaptation to sample shape and size
Optimum process conditions with NO modification of process chamber
Limited cross contamination between processes by using dedicated shuttles
Shuttles for single wafer treatment: 1 x 2”, 1 x 3”, 1 x 4”, 1 x 6”, 1 x 8”
Shuttles for batch processing : 7 x 2”, 3 x 3”
Customized shuttles are available (4” x 4”, 5” x 5”, etc)

## Slide 23: usability corial 210IL

## Slide 24: Process control software
COSMA
The simplest, most efficient software to develop processes, operate, and maintain CORIAL systems
DESKTOP APPLICATION
Process Editing I Process Adjustment I Process Operation I Process Tracability I System Maintenance
MOBILE APPLICATION
Module & Process Follow-Up I Alarms & Warnings Connected Users
NEW
2018
REMOTE CONTROL
COSMA
CORIAL OPERATING SYSTEM FOR MACHINE

## Slide 25: Reprocessing software
COSMA RS
REMOTE
ANALYSIS OF RUNS
DISPLAY UP TO 4
PARAMETERS FROM A RUN
DRAG AND DROP
CURVES TO CHECK PROCESS REPEATABILITY
Simple and efficient software to analyze process runs and accelerate process development

## Slide 26: End point detection
EPD with laser
A CCD camera and laser diode, in the same measuring head, enables simultaneous visualization of the wafer surface and the laser beam impact on it. A 20 µm diameter laser spot facilitates the record of interference signals.
Real-Time etch rate measurement
Real-Time etched depth measurement

## Slide 27: Corial 210IL
ICP-RIE equipment for deep etching applications
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Wide process range for silicon, silicon carbide, glass, sapphire, and quartz deep etch
Support time-multiplexed processes (Bosch) in conventional dry etch reactor
Smaller wafer pieces up to full 200 mm wafer