## Slide 2: Corial 300S
Simple-to-use, manually-loaded batch RIE system
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Wide process range for metal sputtering (Au, Pt, Ti),
and Si, silicon-based compounds (aSi-H, SiO2, Si3N4), polymers etching using fluorinated gases
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Cost-effective mask repair technology with chrome etch capabilities using chlorinated chemistry
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Rapid batch loading of wafers 12x3’’ ; 7x4’’ ; 3x6’’ ; 1x8’’
Loading of glass and quartz masks 2’’x2’’ up to 8’’x8’’

## Slide 3: System description Corial 300S

## Slide 4: System description
General View
960
750
360
1080
600
390
420
490
SMALL FOOTPRINT
0.81 m2
Low CoO

## Slide 5: System description
Detailed View
Pumping system
(TMP 500l/s and dry pump 110m3/h)
Chiller / Heater
RIE reactor
HV and LV power supplies
Process controller
1000 W RF generator
(13,56 Mhz)
Direct loading

## Slide 6: System description
Loading
Direct loading
FAST LOAD AND UNLOAD
< 210 s
LOADING TIME
Shuttle
EASY EXCHANGE BETWEEN SUBSTRATE SHAPE AND SIZE

## Slide 7: Standard rie source corial 300S

## Slide 8: Rie source
Easy-to-use
Heating of the cathode to enhance the desorption of by-products and to improve process performance
Chrome and quartz etch capabilities making the Corial 300S ideal for mask repair applications
Optional end-point detection by laser interferometry for excellent etch control and etch rate determination
Retractable liner for sputter-etch increases time between cleans and reduces clean time
Shuttle (carrier) design, combined with a standard cathode, for a cost-effective and fast reactor adaptation, suitable for multiple applications and substrate types
Simple-to-use reactor with a large cathode that facilitates substrate loading, and substrate holders simply clamped on the cathode without the need for screws or fasteners
Minimized maintenance
HIGH ETCH RATE CAPABILITY

## Slide 9: Rie source
Operation Sequence
TMP
Laser window
Coolant IN
Coolant OUT
Photomask or wafer
A He pressure at 5 Torrs maintains the substrate holder at constant temperature
Helium IN
Substrate
holder
PLASMA
Cathode

## Slide 10: Performances rie processes for mask repair corial 300S

## Slide 11: Rie of chrome for mask repair
Chlorinated chemistry
RIE of Cr on quartz mask
RIE of Cr mask with e-beam PR
Process | Mask | Etch rate (nm/min) | Selectivity (vs mask) | Uniformity (across wafer)
Cr | PR | 50 | 2 | ±3%

## Slide 12: Performances rie processes Corial 300S

## Slide 13: Rie of si, oxides, and nitrides
Fluorinated chemistry
RIE of SiO2 with PR mask – Vertical profile – High etch uniformity
RIE of SiO2– 15 µm deep
RIE of Si3N4 with PR mask
RIE of aSi-H – 300 nm deep

## Slide 14: Rie of metals
Ti Etching with PR mask - Anisotropic profile
Fluorinated chemistry

## Slide 15: High etch rates
Excellent Uniformities
Process | Mask | Etch rate (nm/min) | Selectivity (vs mask) | Uniformity (across wafer)
Polymers | PR | 400 | 1 | ±5%
SiO2 | PR | 50 | 3 | ±3%
Si3N4 | PR | 60 | > 2 | ±3%
Si | PR | 100 | 1 | ±5%
Ti | PR | 25 | 0.3 | ±5%

## Slide 16: Rie source for sputter-etch Corial 300S

## Slide 17: Sputter-etch
RIE Process Chamber for Etching and Sputtering
LINER TO COLLECT ETCH-BY-PRODUCTS AND SPUTTERED MATERIALS
1 min
Reactor Venting
4 min
Pumping down to 10-4 Tor
5 min
Liner replacement
5 min
Plasma cleaning
EASY LINER replacement by a single person
Dedicated process chamber for
Au, Ag, Ni, Fe, Co, Pt, PZT… SPUTTERING

## Slide 18: Sputter-etch
Ar chemistry
Back sputtering of Pt with PR mask
Process | Mask | Etch rate (nm/min) | Selectivity (vs mask) | Uniformity (across wafer)
Au, Pt, PZT, Fe, Co | PR | 45 | > 1 | ±5%

## Slide 19: Shuttle holding approach corial 300S

## Slide 20: Shuttle holding approach
Benefits
Quick adaptation to sample shape and size
Optimum process conditions with NO modification of process chamber
Limited cross contamination between processes by using dedicated shuttles
Shuttles for single wafer treatment: 1 x 8”, 1 x 12”
Shuttles for batch wafer processing : 12x3’’, 7 x 4”, 3 x 6”
Shuttles for photomask repair 2’’x2’’ up to 8’’x8’’

## Slide 21: Shuttle holding approach
Portfolio
5’’x5’’ photomask
6’’x6’’ photomask
7’’x7’’ photomask
carrier for wafer
carrier for photomask
100 mm wafer

## Slide 22: usability corial 300S

## Slide 23: Process control software
COSMA
The simplest, most efficient software to develop processes, operate, and maintain CORIAL systems
DESKTOP APPLICATION
Process Editing I Process Adjustment I Process Operation I Process Tracability I System Maintenance
REMOTE CONTROL
COSMA
CORIAL OPERATING SYSTEM FOR MACHINE

## Slide 24: Reprocessing software
COSMA RS
REMOTE
ANALYSIS OF RUNS
DISPLAY UP TO 4
PARAMETERS FROM A RUN
DRAG AND DROP
CURVES TO CHECK PROCESS REPEATABILITY
Simple and efficient software to analyze process runs and accelerate process development

## Slide 25: End point detection
EPD with laser
A CCD camera and laser diode, in the same measuring head, enables simultaneous visualization of the wafer surface and the laser beam impact on it. A 20 µm diameter laser spot facilitates the record of interference signals.
Real-Time etch rate measurement
Real-Time etched depth measurement

## Slide 26: Corial 300S
Simple-to-use, manually-loaded batch RIE system
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Wide process range for metal sputtering (Au, Pt, Ti),
and Si, silicon-based compounds (aSi-H, SiO2, Si3N4), polymers etching using fluorinated gases
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Cost-effective mask repair technology with chrome etch capabilities using chlorinated chemistry
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Rapid batch loading of wafers 12x3’’ ; 7x4’’ ; 3x6’’ ; 1x8’’
Loading of glass and quartz masks 2’’x2’’ up to 8’’x8’’