## Slide 2: Corial D250 / D250L
PECVD equipment for wafer sizes up to 200 mm
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Large process range for High & Low Temp deposition of silicon compounds
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Designed for NO mechanical cleaning
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Smaller wafer pieces up to full 200 mm wafer

## Slide 3: System description Corial D250 / D250L

## Slide 4: System description
960
750
1080
600
390
General View
THE MOST
COMPACT
MACHINE
ON THE MARKET
30 %
SMALLER FOOTPRINT

## Slide 5: System description
Detailed View
Pumping system
(TMP 350l/s and dry pump 110 m3/h)
EPD with laser
PECVD reactor
HV and LV power supplies
Process controller
Heating controller
300 W RF generator
TMP controller

## Slide 6: System description
960
750
1570
600
390
General View
THE MOST
COMPACT
MACHINE
ON THE MARKET
30 %
SMALLER FOOTPRINT

## Slide 7: System description
Detailed View
Pumping system
(TMP 350l/s and dry pump 110 m3/h)
Load lock
EPD with laser
PECVD reactor
HV and LV power supplies
Process controller
Heating controller
300 W RF generator
TMP controller

## Slide 8: System description
Loading
< 180 s
VACUUM ROBOT ON Corial D250L FOR FAST AND REPEATABLE LOAD AND UNLOAD
< 240 s
LOADING TIME WITH Corial D250
Shuttle
EASY EXCHANGE BETWEEN SUBSTRATE SHAPE AND SIZE

## Slide 9: PECVD reactor Corial D250 / D250L

## Slide 10: Pecvd reactor
RAPID AND UNIFORM DEPOSITION
SiO2 520 nm/min
Si3N4 250 nm/min
SiC 100 nm/minn
…
Precise and uniform temperature control of the substrate and reactor walls delivers excellent deposition repeatability and uniformity
Pressurized reactor ensures high-quality films free of pinholes
Optimized gas showerhead and symmetrical pumping deliver excellent deposition uniformity
High temperature, dual pumped configuration enables efficient plasma cleaning at operating temperature, with no corrosion of mechanical parts
Optimizing film stress control is simple to accomplish thanks to the reactor’s symmetrical design
System can operate for years without the need for manual cleaning

## Slide 11: Pecvd reactor
Flexibility
120 TO 325°C
TEMPERATURE RANGE
0.2 TO 2 T
PRESSURE RANGE
20 TO 150°C
TEMPERATURE RANGE
≤ 65°C
VACUUM VESSEL WALLS

## Slide 12: PECVD reactor
Operation Sequence
1
Substrate Holder
Lift
Vacuum
Chamber
Cathode (Gas shower)

## Slide 13: PECVD reactor
Operation Sequence
2
Lift
Substrate Holder
Cathode (Gas shower)
Vacuum
Chamber
Compressed Air
TMP

## Slide 14: PECVD reactor
Operation Sequence
3
Compressed Air
Lift
Substrate Holder
Heating cable
TMP
Infra-red reflectors
Vacuum
Chamber
Match Box
RF Generator
13.56 MHz
Cathode (Gas shower)
Process Pump
PLASMA
Laser interferometer
Gas Inlet

## Slide 15: Pecvd reactor
Design
IR reflector
Gas shower
Heating cable
Substrate holder
Vertical pipe
High pumping ring

## Slide 16: Pecvd reactor
Standard vs. Pressurized Reactor
Standard PECVD
TMP
PLASMA
Cold walls
300°C
CORIAL Pressurized Reactor
TMP
P2
P1
Roots
PLASMA
Outgasing from the cold walls leads to
film contamination
P1 >> P2 leads to
NO film contamination
(H2O is pumped away by TMP)
H2O
H2O

## Slide 17: Pecvd reactor
Improved Film Quality
1018 C atoms/cm3
1018 O atoms/cm3
5.1017 C atoms/cm3
Very low concentration of O and C atoms in aSi-H films deposited in Pressurized Plasma Reactor
CARBON CONTAMINATION REDUCED BY 5 IN aSi-H FILM
OXYGEN CONTAMINATION REDUCED BY 50 IN aSi-H FILM

## Slide 18: Pecvd reactor
Symmetrical Pumping
SiO2 uniformity
< ±2 %
On 8’’ wafer
Vertical pipe
Gas inlet
Process pump
High pumping ring
Low pumping ring
EXCELLENT DEPOSITION UNIFORMITY

## Slide 19: Pecvd reactor
Symmetrical Design
Cathode area
=
Anode area
Self bias voltage (-VDC).
Zero bias in case of CORIAL reactor
Mean plasma potential (Vp)
When an RF electric field is applied, the plasma potential adjusts itself until it is clamped on the positive portion of RF voltage (At the nearest floating potential (Vf)). The plasma potential is always higher than the highest potential of any surface in contact with the plasma
The mean plasma potential ( Vp ) and the self bias voltage (VDC) accelerate the positive ions and give them a high kinetic energy. In case of pressurized reactor the VDC is zero.
Ion energy is equal to
e∙Vp + Initial energy of positive ions

## Slide 20: Pecvd reactor
Symmetrical Design
Anode area >> Cathode area
Self bias voltage on cathode (VDC) >> 100 V
Mean plasma potential = (VRF – VDC)/2 (≈ few Volts)
Low energy ion bombardment on wafers sitting on the anode (ground)
Anode area = Cathode area
Self bias voltage on cathode (VDC) = 0V
Mean plasma potential = VRF / 2 (Few hundred volts)
High energy ion bombardment on wafers sitting on anode
Cathode
(13.56 MHz)
Anode
Standard PECVD
CORIAL Pressurized Reactor

## Slide 21: Pecvd reactor
Stress Control
Standard PECVD
CORIAL Pressurized Reactor
Double frequency system required for stress control
13.56 MHz for compressive stress
100 to 400 KHz for stress control
  Single frequency convenient for stress control
    13.56 MHz for compressive & tensile stress
PRECISE AND SIMPLE STRESS CONTROL

## Slide 22: Pecvd reactor
Stress Control
Stress controlled by RF power, Ar flow rate and gas mixture
SixNy with tunable stress
SiC with tunable stress
SiO2 with tunable stress

## Slide 23: Performances PECVD processes corial D250 / D250L

## Slide 24: Layer specifications
MEMS
SixNy with tunable stress
SiO2 with tunable stress
SiO2 with breakdown voltage
> 10 MV/cm
Si3N4 with low KOH etch rate
SiO2 with low BOE etch rate

## Slide 25: Layer specificaTions
III-V Compounds, Optoelectronics
DRIE of glass
Low SiO2 BOE etch rate
SiO2 with tunable stress
Si3N4 with low KOH etch rate
Low damaged after annealing
SiC tunable stress

## Slide 26: Layer specifications
Step coverage by
SiH4 + N2O deposition
Step coverage by
HMDSO + O2 deposition
Self-planarized
Deposition of SiOF

## Slide 27: High deposition rates
Excellent Uniformities
Process | Deposition Rate (nm/min) | Refractive Index | Stress (MPa) | Uniformity on 8” Wafers
SiOx | 20 to 500 * | 1.458 to 1.478 | -300 to +50 | < ± 3%
SixNy | 20 to 250 * | 1.8 to 2.1 | -300 to +150 | < ± 3%
SiOF | > 50 | 1.41 ± 0.02 | -100 to -0 | < ± 3%
SiOCH | 50 to 200 | 1.45 ± 0.02 | -100 to -20 | < ± 3%
SixC | 20 to 150 | 2.6 to 2.9 | -100 to +100 | < ± 3%
  Measurement performed with 5 mm edge exclusion
* Configuration-dependent

## Slide 28: Performances time-multiplexed processes Corial d250 with cosma pulse

## Slide 29: COSMA Pulse is the only control software that broadens conventional tools’ process capabilities to enable time-multiplexed processes

## Slide 30: Cosma pulse description
Advanced Process Control
ALL PARAMETERS
CAN BE CONTROLLED AND PULSED
10 ms
DATA AQUISITION
UPGRADE
FOR CORIAL’S SYSTEMS ALREADY INSTALLED AT CUSTOMERS’ SITES
Show/close all the details of the pulsed parameters
Show the pulsed parameters
Mode: Pulsed
Details of the pulsed parameter setting

## Slide 31: Time-multiplexed processes
Example
Enlarged process window to achieve better control of film properties, and supports Atomic Layer Deposition

## Slide 32: Time-multiplexed processes
Performances
Deposition of 30 periods:
6 nm SiO2 + 4 nm aSi-H`
by COSMA Pulse software

## Slide 33: cleaning corial d250 / D250L

## Slide 34: The 200 mm deposition system which never requires mechanical cleaning of reactor or vacuum vessel for many years of operation

## Slide 35: Particle contamination
Reasons for particle contamination:
Films are deposited on cold surfaces (<100°C), giving rise to poor film adhesion responsible for film pealing (big particles, size > 50 µm)
Plasma cleaning cannot fully remove deposited films on cold surfaces, giving rise to built up of thick films and, thereby, film pealing,
Plasma cleaning leads to corrosion of metals other than Al having a high temperature (> 200°C). This corrosion is responsible for big particles (size > 50 µm),
Powders (*) in the plasma responsible for pin-holes in deposited films.
Cathode
(<100°C)
Anode (300°C)
Walls (<60°C)
Standard PECVD
(*) Powders or clusters come from fast exothermic anion-radical reactions as SinHm - + SiHm' to Sin+1Hm+m'-2q- +qH2 that can lead to nucleation of up to 104 Si atoms.

## Slide 36: Reactor plasma cleaning
For Particle Free Processes
HIGH UPTIME
NO MECHANICAL CLEANING
Pressurized
Reactor Design
Automatic
EPD of reactor plasma cleaning process
In situ
Reactor plasma cleaning

## Slide 37: Pecvd reactor
In Situ Cleaning Sequence
1
Roots
Closed gate valve

## Slide 38: Pecvd reactor
In Situ Cleaning Sequence
2
Roots
Closed gate valve
Send N2
P2
P1
SF6
Gas Inlet
N2 leaks
P1 << P2

## Slide 39: Pecvd reactor
In Situ Cleaning Sequence
3
Closed gate valve
Send N2
P2
P1
SF6
Gas Inlet
N2 leaks
P1 << P2
NO fluorine atoms in the vacuum vessel
NO corrosion
PLASMA
Walls at 300°C
Walls at 300°C leads to efficient plasma cleaning and, thereby, minimum particle contamination
SiH4 stopped while plasma still ON
NO pin holes

## Slide 40: usability corial D250 / D250L

## Slide 41: Process control software
COSMA
The simplest, most efficient software to develop processes, operate, and maintain CORIAL systems
DESKTOP APPLICATION
Process Editing I Process Adjustment I Process Operation I Process Tracability I System Maintenance
REMOTE CONTROL
COSMA
CORIAL OPERATING SYSTEM FOR MACHINE

## Slide 42: Reprocessing software
COSMA RS
REMOTE
ANALYSIS OF RUNS
DISPLAY UP TO 4
PARAMETERS FROM A RUN
DRAG AND DROP
CURVES TO CHECK PROCESS REPEATABILITY
Simple and efficient software to analyze process runs and accelerate process development

## Slide 43: End point detection
EPD with laser
Real-Time deposition rate measurement
Real-Time deposition thickness measurement

## Slide 44: Corial D250 / D250L
PECVD equipment for wafer sizes up to 200 mm
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Large process range for High & Low Temp deposition of silicon compounds
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Designed for NO mechanical cleaning
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Smaller wafer pieces up to full 200 mm wafer