## Slide 1
CONTROL OF STRESS
In Corial PECVD SYSTEMS

## Slide 2: Corial pecvd stress control

## Slide 3: Mechanical stress definition
PECVD
Tensile
Compressive
‘Film density’ is lower than the normal value for a selected material
The stress is ‘tensile’ or ‘positive’
‘Film density’ is higher than the normal value for a selected material
The stress is ‘compressive’ or ‘negative’

## Slide 4: Mechanical stress control
PECVD
Mechanical stress in the PECVD films is driven by the film ‘density’ and therefore can be controlled by:
Composition of films, and hence process conditions (gas composition, pressure)
Ion bombardment of films during their growth

## Slide 5: ION bombardment
PECVD
Basic PECVD reactor:
A 13.56 MHz voltage is applied between two electrodes. Electrons, accelerated by the high frequency electric field, ionize the molecules of gas

## Slide 6: ION bombardment
PECVD
Depending on the process conditions (pressure, gas composition, RF power) plasma volume will become positively charged to the ground (plasma potential, Vplasma)
If RF voltage is applied to the substrate holder, then the negative bias voltage will appear (Vbias).
Energy of ions coming to the surface is:
E = e ∙ (Vplasma + Vbias)
RF Voltage
Vplasma
RF Voltage
Time (sec)
RF voltage (V)
Vbias

## Slide 7: Pecvd reactor
CORIAL Symmetrical Design
Cathode area
=
Anode area
Due to the similarity of cathode and anode areas in case of CORIAL reactor, the Vplasma value becomes high.
Simultaneously, no Vbias is created on the substrate holder.
As a result,
Ion energy is equal to
e∙Vplasma
Depending on process conditions
Vplasma can reach several hundreds Volt,
thus providing necessary bombardment for
stress control

## Slide 8: Corial pecvd reactor vs. Standard pecvd
Anode area >> Cathode area
Self bias voltage on cathode (VDC) >> 100 V
Mean plasma potential = (VRF – VDC)/2 (≈ few Volts)
Low energy ion bombardment on wafers sitting on the anode (ground)
Anode area = Cathode area
Self bias voltage on cathode (VDC) = 0V
Mean plasma potential = VRF / 2 (Few hundred volts)
High energy ion bombardment on wafers sitting on anode
Cathode
(13.56 MHz)
Anode
Standard PECVD
CORIAL Pressurized Reactor

## Slide 9: Corial pecvd reactor
Stress controlled in a wide range by RF power, Ar flow rate and gas mixture in a very simple and reproducible manner
SixNy with tunable stress
SiC with tunable stress
SiO2 with tunable stress

## Slide 10: Corial pecvd stress control
Material | Substrate | Stress (MPa) | Deposition rate (nm/min) | Refractive Index | BOE rate (nm/min)
SiO2 | Si | -484 | 79 | 1.46 | 115
 | Si | 32 | 426 | 1.48 | 190
Si3N4 | Si | -706 | 93 | 2.06 | -
 | Si | -365 | 80 | 2.07 | 40
 | Si | 243 | 48 | 1.91 | 144
Some data showing the range of mechanical stress obtained with CORIAL PECVD