## Slide 1
Processing for optical communication devices
In Corial 210IL

## Slide 2: Device structure
quartz wafer
Ge-doped SiO2
PR
PR
Cr
SiO2
quartz wafer
PR
PR

## Slide 3: Process solution Thin SiO2 film etching

## Slide 4: Sample structure
SiO2 Etching Process
Thin SiO2 film etching for channel patterning with
6 µm x 6 µm feature size
6’’ quartz wafer
Ge-doped SiO2 7 µm
PR 0.5 µm
PR 0.5 µm
Cr 0.15 µm – 0.3 µm
SiO2 0.15 µm – 0.3 µm
quartz wafer
PR
PR

## Slide 5: Process requirements
SiO2 Etching Process
Targeted process performances
  Use of C4F8 chemistry
  Minimum CD loss
No damage to underlayer and wafer
  No striation of the sidewalls
  No trenching
  Careful control of etch selectivity
  Etch-stop on Cr layer
Vertical profile (etch slope > 87°)
Process | Etch rate nm/min | Selectivity vs. PR
RIE | 45 | > 2

## Slide 6: Corial process solution
SiO2 Etching Process
PR
SiO2
Cr
Quartz substrate
SiO2
Cr
Mask pattern before etching
  PR stripped by O2 plasma
  Slightly positive profile of PR
Process tuning in RIE mode with wafer fragments
RIE etching on full wafers
1
2
3
No trenching or damage
Vertical profile
Rough surface of Cr revealed
Clean etching
Sharp corners
Process steps

## Slide 7: Corial process solution
SiO2 Etching Process
RIE process performances on 6’’ wafer
Process | Chemistry | Mask | Selectivity to mask | Etch profile | Etch rate (nm/min)
SiO2 etching | C4F8 & O2 | PR | 2.02 | 87° | 49
  C4F8 / O2 gas mixture
  Etching time and overetching duration controlled automatically by laser EPD
  No trenching by the SEM
  Uniform landing all over the wafer (uniformity < 2%) and etch stop on Cr underlayer

## Slide 8: Corial process solution
SiO2 Etching Process
Red curve shows the EPD signal
Overetch
Cr surface is reached
SiO2 etching
Process control by laser interferometry

## Slide 9: Process solution SiO2/GeO2 film etching

## Slide 10: Sample structure
SiO2 /GeO2 Etching Process
Deep Ge-doped SiO2 film etching with SiO2 & Cr mask
quartz wafer
quartz wafer
SiO2
Cr
Ge-doped SiO2

## Slide 11: Process requirements
SiO2 /GeO2 Etching Process
Targeted process performances
  High etching uniformity at ± 3%
  High etch rate
    Process ready for mass production
Minimum CD loss
No damage to wafer
  No striation of the sidewalls
  No trenching
  Careful control of etch selectivity
Vertical profile (etch slope 88.5~91.5°)
Process | Etch rate nm/min | Selectivity vs. mask
ICP-RIE | 550-600 | > 15:1

## Slide 12: Corial process solution
SiO2 /GeO2 Etching Process
Process steps
Mask pattern before etching
SiO2 & Cr mask
Process tuning in ICP-RIE mode with wafer fragments
ICP-RIE etching on full wafers
1
2
3
Vertical etching profile
Clean bottom
No trenching, smooth sidewalls
Smooth bottom
Vertical walls

## Slide 13: Corial process solution
SiO2 /GeO2 Etching Process
ICP-RIE process performances on 6’’ wafer
Process | Chemistry | Mask | Selectivity to mask | Etch profile | Etch rate (nm/min) | Uniformity
SiO2/GeO2 etching | C4F8 & O2 | Cr & SiO2 | > 25 | > 85° | 685 | 1.44
  Deep etching of SiO2/GeO2 with etch depth of 7 µm
  In-situ process control by EPD
  No trenching
  No damage to wafer

## Slide 14: System description corial 210IL

## Slide 15: Corial equipment
Corial 210IL
For up to 200 mm substrates,
Compact footprint,
High power (2 KW) ICP source producing uniform high density plasma,
High power (1 KW) RF source to ensure high etch rates,
Shuttles for efficient adaptation of the tool to different wafer sizes, and soft wafer clamping in ICP-RIE mode,
Quartz liner for fast ICPRIE etching with polymerizing chemistries,
Laser end point detector for measurement of the etching rate and determination of stop-etch point.
This machine can be operated in both RIE and ICP-RIE modes.

## Slide 16: Shuttle holding approach
Corial 210IL
Shuttle WF100
Shuttle NQ200
  Guaranteed no wafer damage due to SOFT wafer clamping