## Slide 1
SiC processing
In Corial 200 series

## Slide 2: Corial solution for SiC processing
200 mm Platform
Single-wafer and batch-loading equipment
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Best-in-class uniformity and process repeatability
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Flexibility and scalability of equipment
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 8.2 | 3.2
Dedicated processes for RF devices, MEMS, power devices…

## Slide 3: Process solution SiC etch

## Slide 4: SiC via etch process
With Ni Mask
ANISOTROPIC ETCH PROFILE
> 1400 NM/MIN
ETCH RATE
> 20 SELECTIVITY TO Ni MASK
± 3 %
UNIFORMITY
SMOOTH
SIDEWALLS
> 100 µm ETCH DEPTH

## Slide 5: Low damage sic etch process
For Power Electronics
SLIGHTLY ISOTROPE ETCH PROFILE WITHOUT CLAMPING
700 NM/MIN
ETCH RATE
2.5 SELECTIVITY TO SiO2 MASK
1:1
ASPECT RATIO
87° PROFILE ANGLE
2.5 µm ETCH DEPTH
NO TRENCHING

## Slide 6: SiC etch process with Ni mask
For MEMS
800 NM/MIN
ETCH RATE
> 25 SELECTIVITY TO Ni MASK
SMOOTH SURFACE
85° PROFILE ANGLE
2 µm ETCH DEPTH

## Slide 7: Tapered Sic etch process
For Power Electronics
TAPERED ETCH PROFILES
250 NM/MIN
ETCH RATE
2
SELECTIVITY TO SiO2 MASK
LOW ROUGHNESS
50° PROFILE ANGLE
2.5 µm ETCH DEPTH

## Slide 8: System description Corial 210IL

## Slide 9: Corial equipment
Corial 210IL
For up to 200 mm substrates,
Hot quartz liners for protection of ICP reactor walls from non-volatile contamination,
High power (2 KW) ICP source producing uniform high density plasma,
High power (1 KW) RF source to ensure high etch rates,
Shuttles for efficient adaptation of the tool to different wafer sizes, and soft wafer clamping in ICP-RIE mode,
Very high conductance pumping system Adixen ATH1600M,
Helium pressure to ensure the thermal transfer between the cathode, the substrate holder and the substrates,
Laser end point detector for measurement of the etching rate and determination of stop-etch point.
This machine can be operated in both RIE and ICP-RIE modes.

## Slide 10: Process solution SiC deposition

## Slide 11: SiC deposition process
High Deposition Rates
Process | Deposition Rate (nm/min) | Refractive Index | Stress (MPa) | WIW Uniformity on 8” wafer (D250) | WIW Uniformity on 4” wafer (D500) | WTW Uniformity on 25 x 4” wafers (D500)
SiC PECVD deposition | 20 to 150 | 2.6 to 3.0 | -100 to +100 | < ± 3% | < ± 1% | < ± 3%

## Slide 12: System description corial D250

## Slide 13: Corial equipment
Corial D250
For up to 200 mm substrates,
Compact footprint,
Uniformly heated pressurized rector design for high uniformity of thickness and deposited film properties,
Film stress control with a single RF frequency,
Efficient plasma cleaning allowing to eliminate manual cleaning,
Laser end point detector for in-situ film thickness control.
This machine can be operated in PECVD mode.