## Slide 1
SiN processing for MEMS type probe card
In Corial 200 series

## Slide 2: Device structure
quartz wafer
Cr pads
quartz wafer
PR
SiN (1 um)
Cr pads
PR
SiN (1 um)
SiN (1 um)

## Slide 3: Process solution sin deposition

## Slide 4: Sample structure
SiN Deposition Process
SiN (1 um)
4’’ quartz wafer (500 um)
Cr pads (1000 Å)
4’’ quartz wafer (500 um)
Cr pads(1000 Å)
4” Quartz wafer patterned with Cr pads

## Slide 5: Process requirements
SiN Deposition Process
High reproducibility
  Run to run ± 5%
High thickness uniformity
  ± 3% on sample
High thickness accuracy
  1 um ± 5%
Process | Deposition rate nm/min | Stress MPa | BOE etch rate nm/min
PECVD | 100 | < +/- 250 | < 100
Targeted process performances

## Slide 6: Corial process solution
SiN Deposition Process
CORIAL PECVD process performances on 4’’ wafer
Process | Chemistry | Deposition rate nm/min | BOE rate nm/min | Stress MPa | Refractive index | Thickness non uniformity | Uniformity WIW | Uniformity Run to Run
1 um SiN deposition | SiH4, NH3 & N2 | > 100 | 72 | -299 +/- 50 | 1.98 +/- 0.01 | 0.1% | 0.96% | 0.38%
  Process conditions: 250°C, Pressure 1000 mTorr, Ar 230 sccm, N2 200 sccm, NH3 150 sccm, SiH4
  In-situ process control by EPD

## Slide 7: Corial process solution
SiN Deposition Process
Process control by laser interferometry
Deposition stop after 1 µm is deposited
Superposition of signals for different runs

## Slide 8: System description corial D250

## Slide 9: Corial equipment
Corial D250
For up to 200 mm substrates,
Compact footprint,
Uniformly heated pressurized rector design for high uniformity of thickness and deposited film properties,
Film stress control with a single RF frequency,
Efficient plasma cleaning allowing to eliminate manual cleaning,
Laser end point detector for in-situ film thickness control.
This machine can be operated in PECVD mode.

## Slide 10: Process solution sin etching with pr mask

## Slide 11: Sample structure
SiN Etch Process
4” Quartz wafer patterned with PR mask
and underlayer Cr
4’’ quartz wafer (500 um)
PR (3 um)
SiN (1 um)
Cr pads (1000 Å)
PR (3 um)
80 um
4’’ quartz wafer (500 um)
PR
SiN (1 um)
Cr pads(1000 Å)
PR
80 um

## Slide 12: Process requirements
SiN Etch Process
  High etching uniformity at ± 3%
  High etch rate
    Process ready for mass production
Minimum CD loss
No damage to underlayer and wafer
  No striations of the sidewalls
  Careful control of etch selectivity
  Etch-stop on Cr layer
Vertical profile (etch slope > 85°)
Process | Etch rate nm/min | Selectivity vs. PR
RIE | 60 | > 2
ICP-RIE | 250 | > 2
Targeted process performances

## Slide 13: Corial process solution
SiN Etch Process
Mask pattern before etching
PR thickness 3 um with slightly positive profile
  Some striation on the walls
Process tuning in RIE mode with wafer fragments
RIE etching on full wafers
Multiple runs
1
2
3
SiN ETCH RIE MODE
No trenching or damage
Vertical profile
Clean corners at the bottom of etched walls
EPD-based adjustment of process duration depending on SiN film thickness

## Slide 14: Corial process solution
SiN Etch Process
CORIAL RIE process performances on 4’’ wafer
Process | Chemistry | Mask | Selectivity to mask | Etch profile | Etch rate (nm/min) | Uniformity
SiN etching | CHF3 & O2 | PR | > 2.6 | > 85° | > 70 | < 1.5
  Process conditions: 50 mTorr, 20°C, RF 150W, CHF3 100 sccm, O2 6 sccm
  In-situ process control by EPD
  No trenching by the SEM
  No damage to Cr underlayer or PR
  Wall roughness as good as PR mask

## Slide 15: Corial process solution
SiN Etch Process
Red curve shows the EPD signal
Laser on PR
Laser on SiN
Overetch
Cr underlayer is reached
SiN etching
Process control by laser interferometry (RIE mode)

## Slide 16: Corial process solution
SiN Etch Process
Mask pattern before etching
PR thickness 3 um with slightly positive profile
  Some striation on the walls
Process tuning in ICP-RIE mode with wafer fragments
1
2
3
ICP-RIE etching on full wafers
Multiple runs
EPD-based adjustment of process duration depending on SiN film thickness
SiN ETCH ICP-RIE MODE

## Slide 17: Corial process solution
SiN Etch Process
CORIAL ICP-RIE process performances on 4’’ wafer
Process | Chemistry | Mask | Selectivity to mask | Etch profile | Etch rate (nm/min) | Uniformity
SiN etching | CHF3 | PR | 2 | > 85° | 380 | < 1.5
  Process conditions: 2 mTorr, 20°C, RF 150W, ICP 650W, CHF3 35 sccm
  In-situ process control by EPD
  Clean etching without residues and particles
  Cr surface reached smoothly

## Slide 18: Corial process solution
SiN Etch Process
Red curve shows the EPD signal
Laser on PR
Laser on SiN
Overetch
Cr underlayer is reached
SiN etching
Process control by laser interferometry (ICP-RIE mode)

## Slide 19: System description corial 210IL

## Slide 20: Corial equipment
Corial 210IL
For up to 200 mm substrates,
Compact footprint,
High power (2 KW) ICP source producing uniform high density plasma,
High power (1 KW) RF source to ensure high etch rates,
Shuttles for efficient adaptation of the tool to different wafer sizes, and soft wafer clamping in ICP-RIE mode
Laser end point detector for measurement of the etching rate and determination of stop-etch point.
This machine can be operated in both RIE and ICP-RIE modes.

## Slide 21: Shuttle holding approach
Corial 210IL
Shuttle WF100
Shuttle NQ200
  Guaranteed no wafer damage due to SOFT wafer clamping

## Slide 22: Cost of ownership corial 210IL

## Slide 23: Throughput and running cost
Corial 210IL
1 x 100 mm wafers per process
Reactor venting – wafer loading & unloading – pumping – process preparation & process end = 180 s;
Etching process = 240 s
Max throughput (8 hours/day, 20 days/month, 95% uptime) = 1350 w/month
Machine uptime 95%
Installation: footprint 1570 mm x 750 mm + dry pump (can be in grey zone)
Gasses: CHF3, O2, He + Exhaust gas scrubbing
Cooling water, CDA, N2
Consumables: 2,000 Euro per year (quartz clamping ring of WF100 shuttle).